Insert the following provisions in the designated location in Part 2 of the casework specification section.

 **2. SOLID LUMBER CORE WORK SURFACE**

 A. Edge Grain Maple Top: [2-1/4"] [1-3/4"] [1"] thick top with edge grain exposed, composed of solid hard maple strips not more than 1-3/4" wide, glued with water resistant resin under heavy pressure side-to-side and end-to-end. Round top edges and corners and sand smooth.

*Following paragraph (linseed oil finish) applies to 2-1/4" and 1-3/4" wood tops only.*

 B. Apply two coats of boiled linseed oil, well rubbed into all surfaces.

Following paragraph (3-coat varnish finish) applies to the 1" thick wood top only.

 B. Apply three coats of moisture and reagent resistant natural varnish finish to top and two coats to underside. Fine sand top between coats.

 END OF APPENDIX A.4